## Slide 1
Capacitance of the
metal-oxide-semiconductor (MOS) structure
Dr. Sanatan Chattopadhyay
Department of Electronic Science
University of Calcutta

## Slide 2
Si based MOS is the key
Microelectronics market
80% is dominated by CMOS
97% is covered by Si
Market
Si is abundant in nature
High quality native oxide (SiO2)
Appropriate mechanical strength
As a material
Applications:
Memory and Storages; Sensors; Diagnostics; Almost in all types of electronic circuits; Filters; Etc. ……..

## Slide 3
Metal-Oxide-Semiconductor (MOS) structure
MOS structure
Schematic view:
A Si substrate (p- or n-type)
SiO2 is grown on it (@800 - 900OC)
Ohmic contacts are taken from the top and bottom
Sometimes, A Poly-Si layer is grown on SiO2, on which gate ohmic contact is taken.
SiO2
Metal
Si-substrate

## Slide 4
Distribution of charges: different biases
P-Substrate
Back contact
Oxide
Gate
Accumulation
VG < 0
+++++++++++
P-Substrate
Back contact
Oxide
Gate
Inversion
VG >> 0
- - - - - - - - - - -
P-Substrate
Back contact
Oxide
Gate
Depletion
VG > 0
-
-
-
-
-
-
Holes are attracted.
Holes are repelled.
Electrons are attracted.

## Slide 5
Band diagram in MOS
Metal
SiO2
Semiconductor
φm
φsi
Ec
EV
EFP
Ei
si
siO2
Metal
SiO2
P-type
Vg < 0
For s<0, accumulation of holes (band bends upward) for p-type substrate.
For s > 0, accumulation of electrons for n-type substrate.
When the band bends downward, s> 0; and when it bends upward, s< 0.

## Slide 6
For charge neutrality of the system, it is required that,
where
QM: charges/unit area on the metal,
Qn: electrons/unit area near the surface (inversion region)
qNAWD: the ionized acceptors/unit area in the space-charge region with depletion width
Qs: total charges/unit area in the semiconductor.
Clearly, in the absence of any work-function difference, the applied voltage will partly appear across the insulator and partly across the semiconductor. Thus,
where Vi, is the potential across the insulator and is given by
Graphical variation of potential, field, charge
WD
Unit area

## Slide 7
Graphical variation of potential, field, charge
Potential
Vox
S
V
0
x
x
0
E (x)
|Qs|/s
x
0
 (x)
|Qs|/s
QM
- Qn
- qNA
Charge distribution.
Electric field distribution
The electric field and potential can be obtained by 1st and 2nd integrations of Poisson’s equation, respectively..
Inversion
Depletion
s
Neutral
EC
EV
Ei
EFP
Band diagram

## Slide 8
Vg = 0
Vacuum
Metal
SiO2
Semiconductor
φm
φs
Ec
EV
EFP
Ei
s
siO2
Metal
SiO2
P-type
Vg > 0
Depth from surface
inversion charge
depletion charge
Inversion
Depletion
s
How does an inversion layer form?

## Slide 9
Metal
SiO2
P-type
Vg > 0
Band diagram at inversion condition
s=0 Flat-band condition
B>s>0 Depletion of holes (bands bending downward)
s=B Fermi-level at mid-gap, EF=Ei(0), np(0)=pp(0)=ni
2B>s>B Weak inversion (electron enhancement)
s>2B Strong inversion [np(0)=pp0+ or NA
Inversion
Depletion
s
B

## Slide 10
Derivation: space charge
Where s is ‘+’ when the band is bent downward, npo and ppo are the equilibrium densities of electrons and holes, respectively, in the bulk of the semiconductor, and
At the surface the densities are:
Redistribution of carriers due to
the application of bias:

## Slide 11
Derivation: space charge
inversion
Strong
:
2
BP
s
y
y
>
inversion
Weak
:
2
BP
s
BP
y
y
y
>
>
.
)
0
(
)
0
(
);
0
(
midgap,
at
level
-
Fermi
:
i
p
p
i
F
BP
s
n
p
n
E
E
y
y
=
=
=
=
downward)
bends
(band
holes
of
Depletion
:
0
s
BP
y
y
>
>
voltage
band
-
Flat
:
0
s
y
=
downward)
bends
(band
holes
of
Accumulation
:
0
s
y
<
From the previous discussions and with the help of the above equations, the following of surface potential can be distinguished:

## Slide 12
Derivation: space charge
The potential (x) as a function of distance can be obtained by using the one-dimensional Poisson’s equation:
Where (x) is the total space-charge density given by:
Now, in the bulk of the semiconductor, far from the surface, charge neutrality must exist.
Therefore at:

## Slide 13
Derivation: space charge
Now,
and,

## Slide 14
Derivation: space charge

## Slide 15
Derivation: space charge
Therefore, the surface field of the MOS structure,
From the surface field, we can deduce the total space charge per unit area by applying Gauss’s law:

## Slide 16
Derivation: space charge
A typical variation of space charge density Qs will be as follows:
i).  is negative: Qs is positive → corresponds to accumulation and function F is dominated by the first term:
ii).  = 0: Qs = 0 → corresponds to flatband condition.
iii). For 2B > s > 0: Qs is negative and we get depletion and weak inversion condition. The function F is now dominated by the second term.
iv). For s > 2B, we will have strong inversion condition with F dominated by the fourth term.

## Slide 17
Derivation: space charge
Also note that this strong inversion begins at a surface potential,
 →
 = 0
|Qs|
(i)
(iv)
(iii)
(ii)
Depth from surface
inversion charge
depletion charge
Inversion
Depletion
s

## Slide 18
MOS - capacitor under accumulation
Accumulation of holes
x
Metal
SiO2
P-type
V
G
p
-
type Si
V
T
C
G
C
ox
V
G
p
-
type Si
V
T
C
G
C
ox
M O S
VG < 0
p-Si
VG < 0; CG = Cox

## Slide 19
MOS capacitor under depletion
Depletion condition: VG > 0
VG > 0
M O S
p-type Si
Depletion of
holes
W
QM
Cox
Cs
V
G
p
-
type Si
V
T
V
G
p
-
type Si
V
T

## Slide 20
MOS capacitor under inversion
Inversion condition s = 2B
VG >>0
M O S
p-Si
Depletion of holes
W
QM
Inversion electrons - function
VG
p-type Si
VT
CG
Low frequency
High frequency
Cox

## Slide 21
Graphical variation of potential, field, charge
The total capacitance C of the system is a series combination of the insulator capacitance
and the semiconductor depletion-layer capacitance CD:

## Slide 22
MOSFET
Vertical Electric Field
Lateral Electric Field
P-Substrate
Back contact
Oxide
Gate
- - - - - - - - - - -
Source
Drain
Channel
MOS
FET
Two orthogonal electric fields work together to initiate the operation of a MOSFET. Vertical field applied from the gate creates a channel for the carriers and lateral electric field drags the carriers from source to the drain, leading to generate a current along the channel.